M. Sc. in Materials Science

Brief Description:

The Department of Metallurgical and Materials Engineering aims to develop a core competence in teaching and research in the areas of Materials Science/Engineering and its applications to defence technologies and products. Being a Defence University, the department offers M. Tech and Ph. D. programs in materials engineering and is also engaged in conducting various short-term courses for DRDO and Defence officers. The main focus of our research is to investigate the structure-property-performance relationship of various materials for Defence applications. To cater to the defence need further, the department offers M.Sc. program in Materials Science for B.Sc. graduates.

This program is offered for DRDO employees and officers from Tri-services, defence public sector undertaking, ISRO/DAE personnel, industry personnel, faculty members from institutes/universities, and civilian students. This program is also open to friendly foreign countries.

At present, the Department is equipped with major characterization facilities (few instrument names are mentioned below) such as:

- High Resolution Transmission electron microscope (TEM) with STEM, Lorentz, HAADF and EDAX facilities

- Field emission scanning electron microscope (FESEM) with EDS

- Small angle x-ray scattering (SAXS)

- Physical Property Measuring System (PPMS)

- Wear and friction measurement equipment

- Micro-Hardness Tester

- Brinell and Rockwell Hardness Tester

- Automatic grinding and polishing machines

- Optical polarizable microscope with image analyser

- Surface Area Analyzer

- Impedance Analyzer and Electrochemical workstation

- Piezometer

- Corona Poling Unit

- UV-Visible Spectroscopy

- Contact Angle measurement unit

and many materials synthesis facilities also available in the Department such as:

- Spray Pyrolysis set-up

- High-Temperature Furnace

- Centrifuge

- Autoclave

- Vacuum Oven

- Orbital Shaker

- Twin screw extruder

- Plastography

- Two roll mill

- Hydraulic press

- Electro spinning unit

- Homogenizer

- Sonicator

The development of know-how and manufacturing technologies of many strategic and advanced materials like intelligent textiles, biosensors, electrospinning, magnetic materials, engineering adhesives, structural composites, hybrid supercapacitors, functional materials, biomaterials for prosthetics, tissue engineering, plastics processing, piezoelectric materials, supercritical foaming technology, additive manufacturing, friction stir processing/welding, crystallographic texture, high entropy alloys, computational materials, batteries etc., are taken up by the faculties and students. The Department is working on many sponsored research projects and the researchers have developed a range of products, including propellers for fuel cells, encapsulated drugs on fibers, magnetic alloys, inorganic oxides for drug delivery, encapsulation and sustained release of anti-cholesterol drugs, polymeric beads and membranes for toxic and heavy metal adsorption (effluent treatment), carbon foams for high-temperature applications and open cell polyurethane foams for automobile applications, development of Ti metal matrix composite, welding of additively manufactured alloys, development of high entropy alloys. Moreover, the Department participates extensively in R&D activities in collaboration with Defence Labs and Establishments of India. International collaborative work is being carried out with Naval Postgraduate School (NPS), California, Cranfield University, UK, Loughborough University, UK, National Ding Hwa University, Taiwan, Weizmann Institute of Science, Israel, etc.

Eligibility:

The eligibility for the M.Sc. postgraduate program is B.Sc./B.Sc. (Honors) or equivalent in any branch of science/mathematics or BE/B.Tech/BS in any branch of Engineering.

Organization:

The program is of four-semester duration with minimum of 80 credits. The first semester is of 20 credits having research methodology as compulsory institutional credit course. The second and third semesters are 20 and 22 credits respectively. In both the semester 3 elective courses (in each semester) are added. Also, one “on job training (OJT)/field project (FP)” is included in second semester.  In third semester research project of 6 credit is added.  In the fourth semester, students will have to perform M.Sc. research project of 18 credits. There will be continuous evaluation in every semester which may comprise two assessments and a final examination for theory subjects. At the end of the final (fourth) semester, students will submit their thesis before going for final evaluation and present their M.Sc. project work before the expert committee (consists of External / Internal members from various R&D Organizations/Institutions / Universities, etc.). No credits are counted for attending an audit course.

Course structure for M.Sc. in Materials Science

Semester I

| Sr. No. | Course Code | Subjects (Theory/Practical) | Contact Hours |  |  | Credits |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | L | T | P |  |
| 1 | MS501 | Structure and Properties of Materials | 3 | 1 | 0 | 4 |
| 2 | MS502 | Materials Characterization Techniques | 3 | 1 | 0 | 4 |
| 3 | MS503 | Thermodynamics, Kinetics, and Phase Transformations | 3 | 0 | 0 | 3 |
| 4 | MS504 | Polymer Synthesis, Manufacturing, and Technology | 3 | 0 | 0 | 3 |
| 5 | MS505 | Materials Laboratory | 0 | 0 | 4 | 2 |
| 6 | RM501 | Research Methodology | 4 | 0 | 0 | 4 |
|  |  | Total |  |  |  | 20 |

Semester II

| Sr. No. | Course Code | Subjects (Theory/Practical) | Contact Hours |  |  | Credits |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | L | T | P |  |
| 1 | MS506 | Processing of Metals and Ceramics | 3 | 0 | 0 | 3 |
| 2 | MS507 | Polymer Processing and Rheology | 3 | 1 | 0 | 4 |
| 3 |  | Elective I | 3 | 0/1 | 0/2 | 3/4 |
| 4 |  | Elective II | 3 | 0/1 | 0/2 | 3/4 |
| 5 |  | Elective III | 3 | 0/1 | 0/2 | 3/4 |
| 6 | OJT/FP | On-Job Training/Field Project | 0 | 0 | 8 | 4 |
|  |  | Minimum Total |  |  |  | 20 |

Semester III

| Sr. No. | Course Code | Subjects (Theory/Practical) | Contact Hours |  |  | Credits |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | L | T | P |  |
| 1 | MS508 | Functional Materials | 3 | 1 | 0 | 4 |
| 2 | MS509 | Principles of Metallurgy | 3 | 0 | 0 | 3 |
| 3 |  | Elective IV | 3 | 0/1 | 0/2 | 3/4 |
| 4 |  | Elective V | 3 | 0/1 | 0/2 | 3/4 |
| 5 |  | Elective VI | 3 | 0/1 | 0/2 | 3/4 |
| 6 | MS541 | Research Project 1 | 0 | 0 | 12 | 6 |
|  |  | Minimum Total |  |  |  | 22 |

Semester IV

| Sr. No. | Course Code | Subjects (Theory/Practical) | Contact Hours |  | Credits |
| --- | --- | --- | --- | --- | --- |
|  |  |  | L | T/P |  |
| 1 | MS542 | Research Project 2 | 0 | 36 | 18 |

Total credit – 18

List of Electives

| Sr. No. | Course Code | Name of the Course |
| --- | --- | --- |
| Electives from the Department |  |  |
| 1 | MS510 | Non-destructive Testing |
| 2 | MS511 | Polymer characterization and Testing |
| 3 | MS512 | Corrosion and Mitigation |
| 4 | MS513 | Nanoscience and Nanotechnology |
| 5 | MS514 | Chemistry of Polymer |
| 6 | MS515 | Additive Manufacturing of Materials |
| 7 | MS516 | Biomaterials |
| 8 | MS517 | Computational Mathematics |
| 9 | MS518 | Computational materials Science |
| 10 | MS519 | Polymer materials and composite blend |

#Since, DIAT adopted choice-based credit system, student can choose any subject from the Institute (other Departments of DIAT) as well as from online platforms (NPTEL, MOOC, SWAYAM, etc.) as an elective subject. A maximum of 6 credits can be opted by student as professional electives from the list of online courses on NPTEL/SWAYAM during second and third semesters.

| Course Code | Subjects (Theory/Practical) | Contact Hours |  |  | Credits |
| --- | --- | --- | --- | --- | --- |
|  |  | L | T | P |  |
| MS501 | Structure and Properties of Materials | 3 | 1 | 0 | 4 |
| Course Objectives: - To introduce the basics of bonding and crystal structure of various crystalline materials - To enable the student to understand the structure and properties of ceramics - To introduce the electronic, magnetic, thermal and optical properties of the materials |  |  |  |  |  |
| Unit I: Introduction, classification of materials; atomic structure, bonding in solids, bonding forces and energies; crystal structure, unit cells, crystal systems, crystallographic points, directions, and planes, Unit II: Crystalline and non-crystalline materials, anisotropy; Structure of crystalline solids: metallic crystal structure Unit III: Ceramic materials, Basic properties, classification of ceramic materials–conventional and advanced, ceramic crystal structure, Defects in ceramics: types of defects, origin of point defects, defects and electron energy levels, defect equillibria in ceramic crystals Unit IV: Electronic and Magnetic Properties: Free electron theory, Fermi energy, density of states, elements of band theory, semiconductors, Hall effect, dielectric behavior, piezo and ferro-electric behaviour, Origin of magnetism in materials, para-, dia-, ferro- and ferri-magnetism Unit V: Thermal and optical properties: Specific heat, heat conduction, thermal diffusivity, thermal expansion, and thermoelectricity, Refractive index, absorption and transmission of electromagnetic radiation, Examples of materials exhibiting the above properties, and their typical/common applications. |  |  |  |  |  |
| Course Outcomes |  |  |  |  |  |
| CO1: Understanding classifications and characteristics of materials CO2: Analysis and properties of crystalline materials CO3: Detailed overview of ceramics and their characteristics CO4: Cognizance of dielectrics, refractories and their applications CO5: Demonstration of Solid state, Sol-Gel, Hydrothermal and Co-precipitation process |  |  |  |  |  |
| Text Book(s): - Materials Science and Engineering by William D. Callister, JohnWiley& Sons, Inc. - Elements of Materials Science and Engineering by Lawrence H. van Vlack. |  |  |  |  |  |
| Reference Book(s): Elements of Ceramics: F.H Norton Fundamentals of Ceramics: Barsoum Introduction to Ceramics: W.D.Kingery Physical Ceramics for Engineers: VanVlack Handbook of Ceramics: Editor S. Kumar Ceramic Materials for Electronics: R.C. Buchanon |  |  |  |  |  |

| Course Code | Subjects (Theory/ Practical) | Contact Hours |  |  | Credits |
| --- | --- | --- | --- | --- | --- |
|  |  | L | T | P |  |
| MS502 | Materials Characterization Techniques | 3 | 1 | 0 | 4 |
| Course Objectives: - To introduce various materials characterization techniques, their basic principles, and capabilities - To enable the student to understand the structure-property relationship of a material through materials characterization - To enable the student to learn and understand the working principle of a few sophisticated instruments through practical demonstration |  |  |  |  |  |
| Unit I: Microscopy and Imaging- Fundamentals of Imaging: magnification, resolution, depth of field and depth of focus, aberration and astigmatism, SEM: imaging modes, image contrast, illustrative applications, Basic principle and components of TEM: Contrast mechanisms, bright field, dark field, TEM application in crystal defect analysis, Electron diffraction in TEM Unit II: Diffraction Techniques- Concepts of diffraction, scattering, and radiation-matter interactions, X-ray diffraction, structure factor determination, phase identification, strain, and crystallite size determination. Unit III: Spectroscopic Techniques- Basis of Spectroscopic analysis, EDS, and WDS applications, X-ray Photoelectron Spectroscopy and Auger electron spectroscopy Unit IV: UV-visible spectroscopy - Beer’s law, Instrumentation, Quantitative analysis; Vibrational spectroscopy- Raman and Infrared, Principles of vibrational spectroscopy, Infrared and Raman activity, Fourier transform infrared spectroscopy, Instrumentation, Applications Unit V: Thermo gravimetric analysis (TGA), Differential thermal analysis (DTA), Differential scanning calorimetry (DSC), Dynamic mechanical analysis (DMA): Basic theory, Instrumentation, and applications. |  |  |  |  |  |
| Course Outcomes CO1: Working principle and capabilities of various characterization techniques CO2: Basics of microscopic and X-ray techniques for materials characterization CO3: Characterization of materials to evaluate structure and properties CO4: Demonstration of microscopic techniques through Lab practicals CO5: Summarizing spectroscopy techniques and their applications |  |  |  |  |  |
| Text Book(s): - Elements of X-ray Diffraction, B. D. Cullity, Prentice Hall, 2001 - Solid State Chemistry and its Applications, Anthony R. West, Wiley. |  |  |  |  |  |
| Reference Book(s): - Materials Characterization, ASM Handbook Vol 10. - Characterization of Materials, Vol 1, Elton N. Kaufmann |  |  |  |  |  |

| Course Code | Subjects (Theory) | Contact Hours |  |  | Credits |
| --- | --- | --- | --- | --- | --- |
|  |  | L | T | P |  |
| MS503 | Thermodynamics, Kinetics, and Phase Transformations | 3 | 0 | 0 | 3 |
| Course Objectives: - To introduce the basic principles of thermodynamic concepts - To impart the knowledge of thermodynamic relations among variables and their transformations - To demonstrate the statistical thermodynamics, free energy equation, and single component system - To introduce the binary system, phases formation, and chemical potential |  |  |  |  |  |
| Unit I: Simple and composite systems, phases, Internal energy, Enthalpy, Entropy, Gibbs Free energy, Specific heat, Laws of thermodynamics, Reversible and Irreversible processes. Generation of Auxiliary Functions: Legendre transforms, Coefficient relations, Maxwell relations, Thermodynamic relations among state functions variables, and its application to solids. Unit II: Free energy of the single component system: Free energy as a function of temperature, Clausius-Clapeyron Equation, Driving force for solidification. Unit III: Solution thermodynamics: Entropy of mixing, Enthalpy of mixing, Free energy of ideal, regular and real solutions, Chemical potential, Unary and binary phase diagrams and Gibbs free energy. Unit IV: Diffusion: Phenomenology, First and Second law of diffusion, Solution to diffusion equations and error function, Types of diffusion Unit V: Solidification of pure metals and alloys, nucleation and growth, diffusional solid-state phase transformations (precipitation and eutectoid), martensitic transformation |  |  |  |  |  |
| Course Outcomes CO1: Understand the basic principles of thermodynamic concepts CO2: Learn the thermodynamic relations among variables and their transformations CO3: Demonstrate basics of statistical thermodynamics CO4: Analysis of free energy equation and curves and their interpretation for a single component system CO5: Detailed understanding of the binary system, phases formation, and chemical potential |  |  |  |  |  |
| Text/References |  |  |  |  |  |
| - M. Modell and R.C. Reid, Thermodynamics and its Applications, Prentice-Hall, Englewood Cliffs, New Jersey, 1983. - H.B. Callen, Thermodynamics and an Introduction to Thermostatics, Jonh Wiley & Sons, New York, 1985. - R.T. DeHoff, Thermodynamics in Materials Science, McGraw-Hill, Singapore, 1993 - Richard E. Dickerson, Molecular Thermodynamics, ‎W. A. Benjamin, 1969 |  |  |  |  |  |

| Course Code | Subjects (Theory) | Contact Hours |  |  | Credits |
| --- | --- | --- | --- | --- | --- |
|  |  | L | T | P |  |
| MS504 | Polymer Synthesis, Manufacturing, and Technology | 3 | 0 | 0 | 3 |
| Course Objectives: - To introduce classifications, properties, and characteristics of various polymers and elastomers - To introduce the chemistry of rubber and their applications - To impart knowledge on the preparation, properties, and applications of high-performance and specialty polymers - To enable the student to understand the types and role of additives and fillers |  |  |  |  |  |
| Unit I: Commodity and general-purpose thermoplastics: Polyethylene, Polypropylene, Polystyrene, Poly vinyl chloride, Polyesters, Acrylic Engineering Plastics: Nylon, Polycarbonate, polysulphones, ABS, Fluoropolymers Thermosetting polymers: Polyurethane, Phenol formlaydehyde, melamine formalydehyde, Epoxy, Unsaturated polyester Unit II: Natural and synthetic rubbers: Recovery of NR hydrocarbon from latex; Styrene butadience rubber, Nitrile, chloroprene rubber, butyl rubber, Silicone, thermoplastic elastomers Unit III: Biopolymers such as cellulosics, poly lactic acid, polyhydroxy butyrate Unit I V: Polymer compounding-need and significance, different compounding ingredients for rubber and plastics (Antioxidants, Light stabilizers, UV stabilizers, Lubricants, Processing aids, Impact modifiers, Flame retardants, antistatic agents. PVC stabilizers and Plasticizers) and their function, use of carbon black, polymer mixing equipment, cross-linking and vulcanization |  |  |  |  |  |
| Course Outcomes CO1: Understanding classifications, properties, and characteristics of polymers and elastomers CO2: Understanding rubber chemistry and uses CO3: Conception of various high-performance and specialty polymers CO4: Cognizance of various additives and fillers CO5: Understanding rubber vulcanization |  |  |  |  |  |
| Text Book(s) - Plastics Materials, 7th Edition, J. A. Brydson, Elsevier |  |  |  |  |  |
| Reference Books: - Textbook of Polymer Science, Fred W. Billmeyer (Wiley) - Polymer alloys and blends by L AUtracki - Polymer nanocomposites: processing, characterization, and applications by Josheph H. Koo (McGraw-Hill Nanoscience and Technology) |  |  |  |  |  |

| Course Code | Subjects (Practical) | Contact Hours |  |  | Credits |
| --- | --- | --- | --- | --- | --- |
|  |  | L | T | P |  |
| MS505 | Materials Laboratory | 0 | 0 | 4 | 2 |
| Course Objectives: - To provide hands on training on various materials characterization techniques - To introduce hands on training on different processes of thin film synthesis - To provide hands on the various processing of polymers |  |  |  |  |  |
| Unit I: Metals polishing and Microstructure analysis, X-ray diffraction characterization and crystal structure determination, Sample preparation and imaging using scanning electron microscopy and interpretation Unit II: Material synthesis by the solid-state method, Nanomaterial synthesis by hydrothermal method, Nano synthesis co-precipitation process, Material synthesis by the sol-gel technique Unit III: Compounding of polymers, Extrusion of polymers and composites, Nanofiber manufacturing by electrospinning |  |  |  |  |  |
| Course Outcomes CO1: Understand Metal polishing and characterization using Optical microscope, Scanning electron microscope and x-ray diffraction CO2: Understand the different synthesis route CO3: Understand the processing of polymers, composite and nanofiber |  |  |  |  |  |
| Text Book(s) - Elements of X-ray Diffraction, B. D. Cullity, Prentice Hall, 2001 - Mechanical Metallurgy, 3rd Ed, George E Dieter, Mc-Graw Hill, New York, 1986. - Manufacturing Processes and Materials for Engineers, L. E. Doyle, 1975. Powder436 - Polymer nanocomposites: processing, characterization, and applications by Josheph H. Koo (McGraw-Hill Nanoscience and Technology) |  |  |  |  |  |
| Reference Book(s) - Materials Characterization, ASM Handbook Vol 10. - Characterization of Materials, Vol 1, Elton N. Kaufmann - Materials Science and Engineering by William D. Callister, JohnWiley& Sons, Inc. |  |  |  |  |  |

| Course Code | Subjects (Theory/Practical) | Contact Hours |  |  | Credits |
| --- | --- | --- | --- | --- | --- |
|  |  | L | T | P |  |
| MS506 | Processing of Metals and Ceramics | 3 | 0 | 0 | 3 |
| Course Objectives: - To introduce the working principles of various processing techniques for metals and ceramics - To impart the processing-structure relationship of various metals and ceramics - To demonstrate specialized techniques such as thin film deposition, sol-gel techniques, co-precipitation, etc. |  |  |  |  |  |
| Unit I: Metallic processing: Casting and forming processes, rolling, forging, extrusion, Heat treatment of Ferrous and Aluminium alloys, Mechanical properties of metals Unit II: Processing of ceramics- Preparation of ceramic powder, Compaction, moulding, sintering, refractory manufacturing processes, Mechanical properties of ceramics Unit III: Thin film deposition: evaporation and sputtering techniques, chemical vapour deposition, thin film growth phenomena Unit IV: Practical: Metal processing- rolling and annealing, sol-gel, co-precipitation |  |  |  |  |  |
| Course Outcomes CO1: Analyse the processing of ceramics CO2: Comprehend the processing of metals CO3: Identify the metal-forming processes CO4: Demonstration of various processing units |  |  |  |  |  |
| Text Book(s): Mechanical Metallurgy, 3rd Ed, George E Dieter, Mc-Graw Hill, New York, 1986. Manufacturing Processes and Materials for Engineers, L. E. Doyle, 1975. Powder436 |  |  |  |  |  |
| Reference Book(s) Metallurgy, Applications, Advantages and Limitations, Klar, Erhard, ASM, 1983, Ohio. Extrusion: the definitive processing guide and handbook, Giles, Harold F.; Wagner, JohnR.; Mount, Eldridge M, 2005. |  |  |  |  |  |

| Course Code | Subjects (Theory/Practical) | Contact Hours |  |  | Credits |
| --- | --- | --- | --- | --- | --- |
|  |  | L | T | P |  |
| MS507 | Polymer Processing and Rheology | 3 | 1 | 0 | 4 |
| Course Objectives: - To introduce the working principles and capabilities of various polymer processing techniques - To introduce the concepts of Newtonian and non-Newtonian fluids and constitutive equations - To familiarize the student with viscoelasticity, rheological measurements, and various models |  |  |  |  |  |
| Unit I: Polymer Processing Compression molding, transfer molding, injection molding, blow molding, reaction injection molding, filament winding, SMC, BMC, DMC, extrusion, pultrusion, calendaring, rotational molding, thermoforming, powder coating, Unit II: Rubber processing in two-roll mill, internal mixer. Unit III: Flow of Newtonian and non-Newtonian fluids, different flow equations, dependence of shear modulus on temperature, molecular/segmental deformations at different zones and transitions. Unit IV: Measurements of rheological parameters by capillary rotating, parallel plate, cone-plate rheometer. Visco-elasticity- creep and stress relaxations, mechanical models, control of rheological characteristics through compounding, rubber curing in parallel plate viscometer, ODR and MDR. |  |  |  |  |  |
| Course Outcomes CO1: Learn the working and principles of polymer processing methods CO2: Understand the rubber processing and rheology CO3: Knowledge of Newtonian and non-Newtonian rheology CO4: Learn the concepts of viscoelasticity and mechanical behavior of polymers |  |  |  |  |  |
| Text Book(s) - Principles of Polymer Processing, 2006, 2nd Edition, Wiley Publisher, Zehev Tadmor, Costas G. Gogos - Rheology Applied in Polymer Processing 1st Edition, 2022, CRC Press by Gupta, B. R. |  |  |  |  |  |
| Reference Books: - Understanding rheology, Oxford University Press, 2001, Faith A. Morrison - Polymer Rheology: Fundamentals and Applications, 2014, Hanser Publisher, Tim A. Osswald and Natalie Rudolph |  |  |  |  |  |

| Course Code | Subjects (Theory) | Contact Hours |  |  | Credits |
| --- | --- | --- | --- | --- | --- |
|  |  | L | T | P |  |
| MS508 | Functional Materials | 3 | 1 | 0 | 4 |
| Course Objectives: - To introduce the fundamentals of functional materials such as the shape memory effect and superelasticity - To impart the concepts of magnetic materials and their applications - To explain the optoelectronic and optical properties of semiconducting materials - To introduce the concepts of metal oxide-based sensors |  |  |  |  |  |
| Unit I: Shape memory and Superelastic alloys: shape memory effect, thermodynamics of martensitic transformation, Stress-induced martensite and superelasticity, Ni-Ti and Ni-Al based alloys and their applications. Unit II: Magnetic materials: Soft and hard magnetic materials, remnant magnetic material, rare earth magnets, Finemet alloys. Unit III: Opto-electronic Materials: Optical properties of semiconductors, absorption and emission processes, Electronic materials such as GaAs and GaN. Unit IV: Sensor: Metal oxide-based sensors, Principles of operation |  |  |  |  |  |
| Course Outcomes CO1: Understand the basics of shape-memory alloys and martensitic transformation CO2: Learn the concepts of magnetic properties of materials CO3: Learn the optoelectronic and optical properties of materials CO4: Knowledge of metal-oxide-based sensing materials and their applications |  |  |  |  |  |
| Text/References Shape memory Materials: K. Otsuka and C. M. Wayman; Cambridge University Press Principles of Electronic Materials and Devices: S. O. Kasap; McGraw Hill Publications |  |  |  |  |  |

Course Name:  Principles of Metallurgy

Course Code: MS509

| Course Code | Subjects (Theory/Practical) | Contact Hours |  |  | Credits |
| --- | --- | --- | --- | --- | --- |
|  |  | L | T | P |  |
| MS509 | Principles of Metallurgy | 3 | 0 | 0 | 3 |

| Course Outcomes (CO): |  |
| --- | --- |
| CO-1: | To understand diffusion in metals and alloys |
| CO-2: | To learn liquid and solid-state transformation in metals |
| CO-3: | To know phases and microstructure of of steel and light alloys |
| CO-4: | To learn various heat treatments of steel and light alloys, and deformation and strengthening concepts. |

|  | Syllabus Details |
| --- | --- |
| Unit I | Diffusion in ideal, nonideal, substitutional and interstitial solid solutions, Fick’s First law, Fick’s second law, Self diffusion in pure metals, diffusion along grain boundaries and free surfaces |
| Unit II | Solidification of metals, crystal growth from the liquid phase, dendritic growth, segregation, solid state transformation, homogeneous nucleation and heterogeneous nucleation |
| Unit III | Phase rule, Phase diagram, Isomorphous alloy systems, The lever rule, Equilibrium heating and cooling of an isomorphous alloy, Microstructure, Eutectic, Fe-FeC diagram |
| Unit IV | TTT and CCT diagrams for carbon steel, Heat treatment of steels, and Aluminum alloys. Deformation and strengthening mechanisms |

Textbooks

- Physical Metallurgy Principles, Robert E Reed-Hill, EWP Pvt, Ltd, 2019

Reference Book(s):

- Mechanical Metallurgy, G.E. Dieter, McGraw-Hill book company, 1988

- Mechanical behaviour of Materials, Williams F Hosford, Cambridge University press, 2005

- Physical Metallurgy, Vijendra Singh, Standard Publishers Distributors, 2010.

| Course Code | Subjects (Theory/Practical) | Contact Hours |  |  | Credits |
| --- | --- | --- | --- | --- | --- |
|  |  | L | T | P |  |
| MS510 | Non-destructive Testing | 3 | 0 | 0 | 3 |
| Course Objectives: - To familiarize the concepts of various non-destructive techniques (NDT) - To enable the student to understand the importance of NDT techniques in detecting cracks and defects - To introduce a few real-time applications of these techniques through case studies |  |  |  |  |  |
| Unit I: Visual Inspection, Liquid Penetrant Testing, Magnetic Particle Testing, Unit II: Eddy Current Testing, Ultrasonic Testing, Unit III: Acoustic Emission Technique, Radiography Technique, Unit IV: Residual Stress Analysis, In-situ Metallography, Automation and Robot in NDT, Unit V: Case study: Grain Size, Weldment, and other Structural Components. |  |  |  |  |  |
| Course Outcomes CO1: Understanding of handy NDT (Non-destructive techniques) CO2: Knowledge of Eddy current and ultrasonic testing CO3: Concept of acoustic emission and radiography techniques CO4: Understanding automated NDT techniques CO5: Case studies on NDT techniques application |  |  |  |  |  |
| Test Book(s) |  |  |  |  |  |
| - Non-destructive Testing of welds, Baldev Raj, C.V. Subramanian and T. Jayakumar, Narosa Publishing House, 2000, Delhi. |  |  |  |  |  |
| Reference book(s) - International Advances in non-destructive testing, (Ed.) W. J. Mcgonnagle, Gordon and Breach Science Publishers, 1981, NY. - Non-destructive Testing, Views, Reviews, Previews, (Ed.) L.L.Alston, Oxford University Press, 1970 - Nondestructive Evaluation and quality control, ASM handbook, Volume 17,ASM International |  |  |  |  |  |

Course Name: Polymer Characterization and Testing

Course Code: MS511

Course Objectives: - To impart knowledge on various physical characterizations of polymers - To introduce various mechanical properties of polymers - To familiarize the thermal and thermo-mechanical properties of polymers - To introduce the optical and electrical properties of polymers

Unit I: Concept of molecular weight distribution and its significance, concept of average molecular weight, determination of number average, weight average, viscosity average and Z-average molecular weights, polymer crystallinity, analysis of polymers using IR, XRD, thermal (DSC, DMTA, TGA), microscopic (optical and electronic) techniques, Molecular wt. distribution: Broad and Narrow, GPC, Mooney viscosity. Polymer solubility and swelling Unit II: Mechanical-static and dynamic, tensile, flexural, compressive, abrasion, endurance, fatigue, hardness, tear, resilience, impact, toughness. Unit III: Conductivity-thermal and electrical, dielectric constant, dissipation factor, power factor, electric resistance, surface resistivity, volume resistivity, Unit IV: Swelling, aging resistance, environmental stress cracking resistance, limiting oxygen index. Heat deflection temperature –Vicat softening temperature, Brittleness temperature, Glass transition temperature, Coefficient of thermal expansion, Shrinkage, Flammability, dielectric constant, dissipation factor, power factor. Unit V: Optical Properties - Refractive Index, Luminous Transmittance and Haze, Melt flow index

Course Outcomes CO1: Understand the molecular weight concepts and physical properties of polymers CO2: Learn the techniques for characterizing various polymer CO3: Understand the mechanical behavior of polymers CO4: Knowledge of thermal and thermo-mechanical properties of polymers CO5: Understand the electrical and optical properties of polymers

Reference Books: - Textbook of Polymer Science, Fred W. Billmeyer (Wiley) - Polymer alloys and blends by L. A. Utracki - Polymer nanocomposites: processing, characterization, and applications by Joseph H. Koo (McGraw-Hill Nanoscience and Technology)

Course Name: Corrosion and mitigation

Course Code: MS512

| Course Outcomes (CO): |  |
| --- | --- |
| CO-1: | Introduction to various forms of corrosion, concept of free energy, partial pressure and related thermodynamics, corrosion mitigation |
| CO-2: | To learn various form of high temperature corrosion |
| CO-3: | Analysis of corrosion data and identify corrosion rate |
| CO-4: | Understand corrosion in various room temperature applications |
| CO-5: | Understand different applications of high temperature corrosion |

|  | Syllabus Details |
| --- | --- |
| Unit I | Introduction to corrosion, Different forms of corrosion, Electrochemical principles of Corrosion, Localized & Metallurgical influenced Pitting, Crevice, Galvanic & Intergranular Corrosion |
| Unit II | Electro chemical impedance, Tafel, Open circuit potential, determination of corrosion rate, defect interactions, scale growth kinetics and mechanisms, Wagner's parabolic scale growth process, other types of kinetics laws and mechanisms, morphological aspects in the growth of thick scales. |
| Unit III | Aspects of thermodynamics, Ellingham diagram various forms of high temperature corrosion including molten salt corrosion, kinetics, transport properties, scale morphologies. |
| Unit IV | Protective Coatings Introduction, coatings & Coating Processes, Supplementary protection systems, Surface preparation. Classification of inhibitors, Corrosion inhibition Mechanism, Selection of an inhibitor system, Cathodic and Anodic Protection principles & classifications. |
| Unit V | Case studies – Corrosion in seawater, Corrosion in steam and gas turbine, Gasifiers and Boilers |

Textbooks

- Per Kofstad, High Temperature Corrosion, Elsevier Applied Science, 1988.

- Mars G. Fontana, Corrosion Engineering, 3rd Ed., McGraw-Hill, Singapore, 1987

Reference Book(s):

- N. Birks and G.H. Meier, Introduction to Oxidation of Metals, Edward Arnold, London, 1983.

- A.S. Khanna, Introduction to High Temperature Oxidation and Corrosion, ASM International, Materials Park, Ohio, 2002.

- Phase transformation in metals and alloys, Porter and Easterling.

Course Name: Nanoscience and Nanotechnology Course Code: MS513

Course Objectives: - To introduce the concepts of nanotechnology and its evolution - To impart knowledge of various nanomaterial and their structure and synthesis - To introduce the properties and characteristics of nano-sized materials - To familiarize the applications and prospects of nanotechnology

Unit I: Overview of Nanostructures and Nanomaterials; Synthesis of Nanomaterials: Types and strategies for synthesis of nanomaterials; Unit II: Crystalline nanomaterials and defects therein; Hybrid nanomaterials; Multiscale hierarchical structures built out of nanosized building blocks (nano to macro); Nanomaterials in Nature: Nacre, Gecko, Teeth; Nanostructures: Carbon Nanotubes, Fullerenes, Nanowires, Quantum Dots. Unit III: Cells response to Nanostructures; Surfaces and interfaces in nanostructures, Ceramic interfaces, Superhydrophobic surfaces, Grain boundaries in Nanocrystalline materials, Unit IV: Thermodynamics of Nanomaterials; Overview of properties of nanostructures and nanomaterials; Overview of characterization of nanostructures and nanomaterials Unit V: Applications of Nanotechnology in various fields

Course Outcomes CO1: Knowledge of the basics of nanotechnology CO2: Understanding the behavior of materials in the nano-scale CO3: Learn the synthesis and properties of nanomaterials CO4: Knowledge of the application of nanotechnology

Text Book(s) T. Pradeep, NANO: The Essentials,Tata McGraw-Hill Publisher, 2007. ISBN-13:978- 0-07-061788-9.

Reference Book(s) K. Haghi, G. E. Zaikov, Advanced Nanotube and Nanofiber Materials, Nova Science Publishers Inc, 2012 Vladimir V. Mitin, Viatcheslav A. Kochelap, Michael A. Stroscio, Introduction to Nanoelectronics: Science, Nanotechnology, Engineering, and Applications, Cambridge University Press, 2008

Course Name: Chemistry of Polymers

Course Code: MS514

Course Objectives: - To introduce various polymerization methods and their kinetics - To familiarize the student with the polymerization techniques - To impart the knowledge of block- and graft-co-polymers - To introduce the structure-property relationship in polymers

Unit I: Chemistry of High Polymers Monomers, functionality, degree of polymerizations, classification of polymers, glass transition, melting transition, criteria for rubberiness. Unit II: Polymerization methods: addition and condensation; their kinetics, metallocene polymers and other newer methods of polymerization, copolymerization, monomer reactivity ratios, and its significance, kinetics, different copolymers, random, alternating, azeotropic copolymerization. Unit III: Block and graft copolymers, techniques for polymerization: bulk, solution, suspension, emulsion. Unit IV: Concept of intermolecular order (morphology) – amorphous, crystalline, orientation states. Factor affecting crystallinity. Crystalline transition. Effect of morphology on polymer properties.

Course Outcomes CO1: Understand the basics of polymerization reactions and their kinetics CO2: Knowledge of polymerization techniques and their applications CO3: Learn the concepts of block- and graft-co-polymers CO4: Understand the fundamentals of structure-property relationship

Reference Books: - Textbook of Polymer Science, Fred W. Billmeyer (Wiley) - Polymer alloys and blends by L AUtracki - Polymer nanocomposites: processing, characterization, and applications by Josheph H. Koo (McGraw-Hill Nanoscience and Technology)

| Course Code | Subjects (Theory/Practical) | Contact Hours |  |  | Credits |
| --- | --- | --- | --- | --- | --- |
|  |  | L | T | P |  |
| MS515 | Additive Manufacturing of Materials | 3 | 0 | 0 | 3 |
| Course Objectives: - To introduce the concepts of additive manufacturing techniques - To familiarize with the liquid and solid-state additive manufacturing - To impart knowledge of various types of additive manufacturing and their capabilities and limitations - To introduce case studies related to polymer, ceramics, and metal additive manufacturing |  |  |  |  |  |
| Unit I: Basic Introduction Overview- History- Need classification- Additive Manufacturing Technology in product development- Materials for Additive Manufacturing Technology- Tooling- Applications Unit II: Solid and liquid-based additive manufacturing Classification – Liquid-based system- Stereolithography Apparatus (SLA)- Principle, process, advantages, and applications – Solid-based system- Fused Deposition Modeling- Principle, process, advantages and applications, Laminated object Manufacturing. Unit III: Powder-based additive manufacturing Selective Laser Sintering- Principles of SLS process- Process, advantages and applications, Three-Dimensional Printing – Principle, Process, advantages and applications- Laser Engineered Net Shaping (LENS), Electron Beam Melting. Unit IV: CASE STUDIES Case studies for metals and alloys, Ceramics and Polymers |  |  |  |  |  |
| Course Outcomes CO1: Knowledge of basics and application of additive manufacturing CO2: Understanding liquid and solid-state additive manufacturing CO3: Concepts of various types of additive manufacturing and challenges CO4: Case studies on metal, ceramic and polymer additive manufacturing |  |  |  |  |  |
| Test Books: - Chua C.K., Leong K.F., and Lim C.C., “Rapid prototyping: Principles and applications”. Third Edition, World Scientific Publishers, 2010. - Gebhardt A., “Rapid prototyping”, Hanser Gardener Publications, 2003. |  |  |  |  |  |
| Reference Books: - Liou L.W. and Liou F.W., “Rapid Prototyping and Engineering applications: A tool box prototype development”, CRC Press, 2007. - Kamrani A.K. and Nase E.A., “Rapid Prototyping: Theory and practice: Springer, 2006. - Hilton P.D. and Jacobs P.F., “Rapid Tooling: Technologies and Industrial Applications”, CRC press, 2000. - Dougles Bryden, “CAD and Prototyping for Product Design”, 2014 |  |  |  |  |  |

Course Name: Biomaterials Course Code: MS516

Course Objectives: - To introduce the basics of biomaterials and the related concepts - To familiarize the student with different classes of biomaterials - To introduce the concepts of nano-biomaterials and their properties - To impart knowledge on various processes used for manufacturing biomaterials

Unit I: Introduction to biomaterials, Tissue Engineering, Biocompatibility, Biodegradation Biofluids and medical devices, Biostructures Unit II: Ceramic-based biomaterials, metallic biomaterials, polymer-based biomaterials, Biofluidic, medical devices, Biostructures Unit III: Nano-biomaterials: Self-assembly of nanomaterials, hydrophilic, hydrophobic and surfaces, biomimicking Unit IV: Medical imaging, electrospinning of scaffold structures, Additive manufacturing of medical devices, biofluidics and biostructure Unit V: Case studies: Lotus leaf, Gecko feet, Nacre/Bone. Application of nanocomposite biomaterials: artificial biomaterials, antidrug coatings, self-cleaning surfaces, sensors, Riboswitches

Course Outcomes CO1: Knowledge of biomaterials, biocompatibility, and tissue engineering CO2: Learn the different classes of biomaterials and their properties CO3: Understand the nano-biomaterials and their properties CO4: Knowledge of biomaterials manufacturing processes

Text Book(s): Biomaterials- An Introduction, Joon Park- Publisher Springer423

Reference Book(s): Biomaterials- Principals and Applications- Joon Park- CRC Press Handbook of Biomaterial Properties- Garth Hastings- Springer Handbook of Biomaterials Properties- William Murphy- Springer Handbook of Biomaterial Properties- Jonathan Black- Chapman and Hal

| Course Code | Subjects (Theory/Practical) | Contact Hours |  |  | Credits |
| --- | --- | --- | --- | --- | --- |
|  |  | L | T | P |  |
| MS517 | Computational Mathematics | 3 | 0 | 0 | 3 |
| Course Objectives: - To lay the foundation of linear algebra that is necessary for scientific computing - To extend the knowledge to multivariable calculus - To familiarize the students with vector calculus - To demonstrate the fundamentals of numerical methods applied to engineering problems |  |  |  |  |  |
| Unit I: Linear Algebra: Algebra of real matrices: Determinant, inverse, and rank of a matrix; System of linear equations (conditions for unique solution, no solution and infinite number of solutions); Eigenvalues and eigenvectors of matrices; Properties of eigenvalues and eigenvectors of symmetric matrices, diagonalization of matrices; Cayley-Hamilton Theorem. Unit II: Calculus of single and multiple variables: Limit, Continuity and differentiability; Maxima and minima; Partial derivatives; Total derivative. Unit III: Vector Calculus: Gradient, divergence and curl; Line integrals, and Green’s theorem. Unit IV: Numerical Solution of Differential Equations: Concepts of discretization in space/time, implicit, explicit; Taylor’s series; Solution to ODEs; Classification of second order linear partial differential equations; Method of separation of variables: One-dimensional heat equation and two-dimensional Laplace equation. |  |  |  |  |  |
| Course Outcomes CO1: Understand the basics of Linear Algebra CO2: Recognize the principles of advanced calculus CO3: Introduce vector calculus CO4: Utilise numerical methods to solve differential equations |  |  |  |  |  |
| Text Book(s) - Advanced engineering mathematics: Kreyszig; Wiley. - Advanced engineering mathematics: Jain/Iyenger; Narosa |  |  |  |  |  |
| Reference Book(s) - Advanced engineering mathematics: Peter V. O’Neil Cengage Learning - Advanced engineering mathematics: Alan Jeffery; Academic Press - Calculus and analytic geometry: Thomas/Finney; Narosa - Numerical methods for Engineers: Steven C. Chapra and Paymond P. Canale |  |  |  |  |  |

| Course Code | Subjects (Theory/Practical) | Contact Hours |  |  | Credits |
| --- | --- | --- | --- | --- | --- |
|  |  | L | T | P |  |
| MS518 | Computational Materials Science | 3 | 0 | 0 | 4 |
| Course Objectives: - To revisit and build up on the programming skills - To familiarise students with modeling and simulation by simple models - To demonstrate the multi-scale models employed in materials engineering - To introduce data-driven modeling |  |  |  |  |  |
| Unit I: Review of programming in high-level and low-level languages Unit II: Lotka-Volterra Model: Analytical and Numerical Solution; Solving Fick’s laws of Diffusion numerically in 1D using low-level language; Diffusion in 3D using advanced solvers; Random Walker model Unit III: Monte Carlo method; Ising Model; Sharp and Diffuse interface models; Phase field method for the evolution of microstructure: Cahn-Hilliard and Allen-Cahn model. Unit IV: Introduction to Machine Learning: Supervised and Unsupervised models, Fitting and visualization of multidimensional data; Data analytics using principal component analysis |  |  |  |  |  |
| Course Outcomes CO1: Understand the basics of programming CO2: Implement the analytical and numerical solution to partial differential equations utilized in materials science CO3: Analyze the mesoscopic modelling techniques CO4: Understand the principles of data-driven modeling |  |  |  |  |  |
| Text Book(s): - Introduction to Computational Science: Modeling and Simulation for the Sciences, Princeton University Press, A. B. Shiflet and G. W. Shiflet - Introduction to Computational Materials Science – Richard LeSar, Cambridge University Press |  |  |  |  |  |
| Reference Book(s): - Computational Materials Engineering: An Introduction to Microstructure Evolution, Elsevier Academic press, K. G. F. Janssens, D. Raabe, E. Kozeschnik, M. A. Miodownik, B. Nestler - David V. Hutton, Fundamentals of Finite Element Analysis - Mathematic physics (V. Balakrishnan) - Numerical Recipes in C(William H. Press, Vetterling, Teutolsky, Flannery) |  |  |  |  |  |

| Course Code | Subjects (Theory/Practical) | Contact Hours |  |  | Credits |
| --- | --- | --- | --- | --- | --- |
|  |  | L | T | P |  |
| MS519 | Composite Materials and Polymer Blends | 3 | 0 | 0 | 3 |
| Course Objectives: - To introduce the concepts of composite materials and their types, matrices, and reinforcements - To impart the knowledge of various filler-reinforced polymer composites, their processing techniques, and the mechanics of composites - To introduce preparation and properties of metal-matrix and ceramic-matrix composites - To introduce the concepts of polymer blends and their thermodynamics of miscibility |  |  |  |  |  |
| Unit I: Matrix, reinforcement, types of reinforcing fillers, continuous and discontinuous fibers, carbon, glass, aramid, and other fibers, preparation methods and properties, particulate fillers, dispersion and interfacial phenomena, nanofillers, functional fillers. Unit II: Polymer Matrix Composites: Polymer resins – thermosetting resins, thermoplastic resins – reinforcement fibers – rovings -woven fabrics – nonwoven random mats – various types of fibers. PMC processes – hand layup processes – spray up processes – compression molding – reinforced reaction injection molding – resin transfer molding – Pultrusion – Filament winding – Injection molding. Fiber-reinforced plastics (FRP), Glass Fibre Reinforced Plastics (GFRP). Mechanics of Composites, basic constitutive equations, rule of mixture, Halpin-Tsai equations etc. Applications of PMC in aerospace, automotive industries Unit III: Metal Matrix Composites: Characteristics of MMC, various types of metal matrix composites alloy vs. MMC, advantages of MMC, limitations of MMC, Reinforcements – particles – fibers. Effect of reinforcement – volume fraction – rule of mixtures. Processing of MMC – powder metallurgy process – diffusion bonding -stir casting – squeeze casting, a spray process, Liquid infiltration In-situ reactions-Interface-measurement of interface properties- applications of MMC in aerospace, automotive industries Unit IV: Ceramic matrix composites, carbon-carbon composites, processing, manufacturing, properties, and applications in aerospace and automotive components Unit V: Introduction to polymer blends, nanostructured materials and nanocomposites, Thermodynamics of polymer blends, mixing, factors governing miscibility, immiscible polymers, and phase separation. Influence of interface on the property of blends and nanocomposites. Compatibilizers and compatibilization. Blends of amorphous & semi-crystalline polymers, inter-penetrating networks, thermoplastic and thermoset blends, rubber-toughened polymers, and particulate and fiber-reinforced composites. |  |  |  |  |  |
| Course Outcomes CO1: Understanding of various reinforcements and matrices CO2: Knowledge of the role of interface in mechanical properties CO3: Understanding fiber-reinforced composites and challenges CO4: Knowledge of composite processing methods CO5: Understanding of polymer nanocomposites and blends |  |  |  |  |  |
| Text Books: - Mathews F. L. and Rawlings R. D., Composite Materials: Engineering and Science, 1st Edition, Chapman and Hall, London, England, 1994. - Chawla K. K., Composite Materials, Second Edition, Springer – Verlag, 1998. - Introduction to Materials Engineering, William Callister - Polymer alloys and blends by L AUtracki |  |  |  |  |  |
| Reference Books: - Clyne, T. W. and Withers, P. J., Introduction to Metal Matrix Composites, Cambridge University Press, 1993. - Strong, A.B., Fundamentals of Composite Manufacturing, SME, 1989. - Sharma, S.C., Composite Materials, Narosa Publications, 2000. - Broutman, L.J. and Krock,R.M., Modern Composite Materials, Addison-Wesley, 1967. - ASM Hand Book, Composites, Vol.21, ASM International, 2001. |  |  |  |  |  |